## Slide 1: Coupled cluster methods in the condensed phase
Garnet Kin-Lic Chan California Institute of Technology

## Slide 2: Molecular simulations are precise
in small molecules, theory can rival or replace expt
increase basis size
higher level correlation treatment
Watson and Chan, JCTC, 8, 4013 (2012)
Butadiene: C4H6 optical excitation
theory: 6.11 +/- 0.02 eV
expt 6.01 +/- 0.05 eV
theory and expt agree perfectly within error bars (2s)

## Slide 3: Materials simulations are not!
in materials, simulations are more of a “suggestion”
Are systematic, precise, predictive simulations of materials, as
currently exist in molecules, possible?

## Slide 4: How to obtain high precision?
QED: fine-structure constant
experiment (2011)
theory (2012)
up to 10th order Feynman diagrams
in principle, this approach can be used in materials!

## Slide 5: Coupled cluster theory
P
P
H
H
P
H
P
H
P
H
CCSD sums all (products of)
diagrams with 2p-2h
intermediate lines
CCSDT sums all (products of)
diagrams with 3p-3h
intermediate lines
all rings, ladders, additional
lowest order Parquet terms
CCSD(T): gold standard
of molecular QC
quant. chem. has systematic machinery to resum diagrams

## Slide 6: Coupled cluster in solids: total energies
sum over all dimers,
trimers etc. ...
OSV-L-CCSD(T) with CCSDT(Q) / DMRG corrn.
aug-cc-pVTZ basis with F12 geminals
lattice energy 55.97 ± 0.76 ± 0.1 kJ/mol
better than 1 kJ/mol accuracy –
similar to best calcs in molecules
how well can we determine
lattice energy of benzene crystal?
Yang, Hu, Usvyat, Matthews,
Schuetz, Chan, Science (2014)

## Slide 7: Coupled cluster in solids: spectra
what is the spectral function of the
uniform electron gas?
compare to: GW, DMRG (where possible)
equation of motion CC (EOM-CC): systematic
diagrammatic approximations to Green’s function

## Slide 8
14e, 19 orbital UEG
k = (0, 0, 0) rs=4
McClain, Lischner, Watson, Matthews,
Ronca, Louie, Berkelbach, Chan, PRB (2016)
EOM-CCSDT, DMRG
perfect agreement
GW completely
depends on
starting point
(CC completely
invariant)
GW + C
predicts
spurious peaks

## Slide 9
114e, 485 orbital UEG
k = (0, 0, 0) rs=4
(EOM) coupled cluster: quantitative treatment of core
excitations in metallic sodium!
Na photoelectron spectrum

## Slide 10
brief interlude

## Slide 11
Coupled cluster theory appears promising
for condensed phase simulations
The main barrier is the lack of technical
infrastructure to develop quantum
chemistry in the condensed phase!
These methods have existed for molecules
for a long time
Why have they not been explored in crystals?

## Slide 12: Standing on the shoulders of giants
correlation methods
integral transformations / RI / CD
Hartree-Fock
integrals
basis sets
basis functions

## Slide 13: The PBC module of PySCF
PBC integral transformations / RI / CD
PBC Hartree-Fock
PBC integrals
PBC basis sets
PBC basis functions
scaling the pyramid so you don’t have to

## Slide 14: PySCF
Performance
Complexity
Features
pyscf.org
Qiming Sun, lead developer

## Slide 15: PySCF: molecular code performance
CASSCF up to 3000 fns
HF/DFT up to 5000 fns
CC up to 1500 fns
HF, DFT, TD-DFT, MP2, CCSD(T),
EOM-CCSD, CASSCF, NEVPT2,
FCI, DMRG, DMRG-PT2
relativistic 2C/4C HF/DFT
gradients: HF/DFT/MP2/CCSD(T)
NMR, properties, solvation ...
and much more ...

## Slide 16: PySCF: extreme simplicity
 | Python | C
Overall | 60.3 k | 26.2 k
DFT | 4.1 k | 7.3 k (LebedevGrid 5k)
MCSCF | 5.9 k | 50
CCSD | 0.7 k | 0
PySCF = mainly Python + a little C + 3 external libraries
(hdf5, libcint, libxc)
total lines of code

## Slide 17: Simple code + hand-tuned performance
NEVPT2
everything is einsum
high-performance integral and tensor contraction kernels
AVX2/AVX-512
integral kernel
TBLIS tensor
contraction
(Devin
Matthews)

## Slide 18: Use same code for molecule and solid
import pyscf.pbc.gto
from pyscf import mp, cc, mcscf cell = pyscf.pbc.gto.M(...) eri = ao2mo.get_ao_eri(cell)
mf = scf.RHF(cell).run()
print mp.MP2(mf).kernel()[0] print cc.CCSD(mf).kernel()[0] mc = mcscf.CASSCF(mf, 8, 8) print mc.kernel()[0] td = tddft.TDHF(mf) print td.kernel()[0]
import pyscf.gto
from pyscf import mp, cc, mcscf mol = pyscf.gto.M(...) eri = ao2mo.get_ao_eri(mol)
mf = scf.RHF(mol).run()
print mp.MP2(mf).kernel()[0] print cc.CCSD(mf).kernel()[0] mc = mcscf.CASSCF(mf, 8, 8) print mc.kernel()[0] td = tddft.TDHF(mf) print td.kernel()[0]
Exactly the same implementation!
Notes: The difference is the initialization, cell or mole

## Slide 19
back to coupled
cluster calculations
in the condensed phase

## Slide 20: Ground-state CCSD: covalent solids
TZVP basis 4x4x4 mesh (energy) 3x3x3 mesh (props)
VASP
Booth, Grueneis, Kresse, Alavi, Nature (2013)
McClain, Berkelbach, Sun, Chan, JCTC (2017)

## Slide 21: EOM-CCSD: Si band structure
 | LDA | GW | CCSD | Expt
direct | 2.49 | 3.4 | 3.2 | 3.1—3.4
indirect | 0.54 | 1.20 | 1.19 | 1.17
IP/EA-EOM CCSD / (TZVP) 4x4x4 k-pt mesh
failure of LDA for Si bandgap - poster child of “bandgap” problem
success of GW for this led to its acceptance
EOM-CCSD bandgaps are good!

## Slide 22: EOM-CCSD: Si band structure
3x3x3 shifted k-pt mesh

## Slide 23: Semiconducting bandgaps
EOM-CCSD better than G0W0, similar to GW0

## Slide 24: The story of diamond
C bandgap (pre-2010)
expt | 5.48 eV
DFT/HSE | 5.49 eV
G0W0 | 5.50 eV
GW0 | 5.68 eV
CCSD (2017) | 5.37 eV
bandgap appears under control
2010: Giuistino et al: ZPE correction ~ 0.6 eV (others 0.4-0.6 eV)
true bandgap ~ 6 eV, underestimated by all methods by 0.5 eV!
TZVP
DZVP

## Slide 25: Systematically achieving high precision
Is there a (T)
correction for spectra?
EOM-CCSD*
EOM-CCSD*:
correction is
in wrong direction!
Stanton, Gauss (1996)
CC: in principle, add next order terms, CCSDCCSDT!
but, full T term is too expensive.
g.s. approximate T by (T). This is the “gold-standard”.

## Slide 26: The shame of EOM-CCSD* (GW100 set)
EOM-CCSD* is a terrible (T) correction: worse than EOM-CCSD!

## Slide 27: Formulating (T) correctly for spectra
g.s. CCSD(T): right EOM eigenvector as approx to left.
insert same approx for IP/EA-EOM-CCSD* ...
MAE: EOM-CCSD* 149 meV EOM-CCSD4 55 meV!

## Slide 28: Converging diamond with “triples”
estimated TZVP gap: 6.1 eV
exptal gap – ZPE : 6.0-6.1 eV
towards fully converged excitation energies in solids!
McClain, Chan
in preparation

## Slide 29: Beyond energies and spectra
CC theory is a systematic framework to generate
and resum zero-temperature diagrams
but diagrams can be re-interpreted as finite-temperature
diagrams, or diagrams on Keldysh contour
opens route to CC for systematic treatment
of finite-temperature and non-equilibrium phenomena
White and Chan, in preparation

## Slide 30: Semiconducting bandgaps
EOM-CCSD better than G0W0, similar to GW0

## Slide 31: Transition metal dichalcogenides
main uncertainty - TDL extrapolation from: 7x7 EOM-CCSD
*with SOC correction
similar gaps to G0W0
Pulkin, Chan, in preparation
expt: MoS2 gap:
direct  indirect
under small strain
theory: direct, indirect gaps
almost degenerate

## Slide 32: Nickel oxide

## Slide 33: Finite temperature CC

## Slide 34: Conclusions
Accessible infrastructure exists to develop
quantum chemistry in the condensed phase
Coupled cluster, with the correct “triples” will
provide gold standard for condensed phase spectra
Coupled cluster techniques may be generalized to
beyond electronic structure and spectra