## Slide 1
Equations of State
Ronald Cohen
Geophysical Laboratory
Carnegie Institution of Washington
cohen@gl.ciw.edu
2012 Summer School on Computational Materials Science Quantum Monte Carlo: Theory and Fundamentals
July 23–-27, 2012 • University of Illinois at Urbana–Champaign
http://www.mcc.uiuc.edu/summerschool/2012/
QMC Summer School 2012 UIUC

## Slide 2: Need for Equations of State
QMC gives us the energy at a set of points for different structures and volumes
To predict phase stability and to compare with experiment we need the pressure
The most stable phase has the lowest free energy, or at zero temperature, the lowest enthapy.
The relationship among E, V, P, and T is the equation of state.
Also enthalpy H=E+PV and free energy G=H-TS
Cohen, R. E. & Gulseren, O. Thermal equation of state of tantalum. Phys. Rev. B 63, 224101-224111 (2000).
Ta Thermal equation of state

## Slide 3: Pressure vs. volume Ta isotherms

## Slide 5: Residuals for T=0 isotherm: Evidence for electronic transition

## Slide 6: Ta bands and DOS
V=12.66 Å3 (5 GPa)
V=9.3 Å3 (460 GPa)

## Slide 7: Vinet parameters vs. temperature

## Slide 8: Thermal pressure vs. V

## Slide 9: Thermal pressure vs. T

## Slide 10: Average Thermal Pressure

## Slide 11: Simple Equation of State for Ta
P (GPa) = P0K+Pth
P0K is Vinet equation:
x=(V/V0)1/3
P=3 K0 (1-x) exp (3/2 (K0’-1) (1-x))/x2
with V0=123.632 K0=190.95 K0'=3.98
Pth = 0.00441 T
This should be good to better than ±5 GPa to 9000 K and for V>80 bohr3 (35% compression).

## Slide 12: An accurate high temperature global equation of state
T=0 Vinet isotherm
V dependent Thermal Pressure
Heat Capacity

## Slide 13: Global free energy fit

## Slide 19: cBN Raman Frequencies
Within harmonic approx. DFT frequency is reasonable
But, cBN Raman mode is quite anharmonic
With anharmonic corrections, DFT frequencies are not so good.
Compute energy vs. displacement with DMC and do 4th-order fit. Solve 1D Schrodinger eq. to get frequency
Anharmonic DMC frequency is correct to within statistical error

## Slide 20: Summary
Fit your DFT and QMC results to equations of state, carefully.
Much can be learned from the equation of state, and the parameterizations are very useful, particularly for comparing with experiments or input to other studies.